# General Characteristics of Common Blue Pigments

| Pigment | Composition | CI numbers | Usage | Density | Refractive Index | Microscopic characteristics | Other characteristics | Health |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| aniline blue | triarylmethane dye | CI 42780; Solvent Blue 3 | patented in January 1861 |  |  | reacts with collagen to produce a blue-green fluorescence | water soluble; used for inks and for dying wool, nylon, leather, wood, and paper | toxic by ingestion |
| azurite | natural basic copper carbonate, 2CuCO3-Cu(OH)2 | Pigment Blue 30; CI 77420 | since antiquity | 3.77-3.80 | 1.730; 1.838; 1.758 | strong birefringence; highly refracting; particles are irregular in size with fractured edges; pleochroic from pale blue to deep blue | decomposes in acids evolving CO2; turns black with warm alkalis, hydrogen sulfide or sulfur fumes | chronic exposure may cause anemia |
| blue verditer | synthetic blue copper carbonate, 2CuCO3-Cu(OH)2 | Pigment Blue 30; CI 77420 | European recipes date to medieval times | 3.8 | 1.730; 1.838; 1.758 | strong birefringence; highly refracting; fine grain spheres occur as aggregates; pleochroic from pale blue to deep blue | decomposes in acids evolving CO2; turns black with warm alkalis, hydrogen sulfide or sulfur fumes | chronic exposure may cause anemia |
| cerulean blue | cobalt tin oxide, CoO-nSnO2 | Pigment Blue 35; CI 77346; CI 77368 | developed in 1805, first sold in 1860 |  | 1.78 - 1.84 | very fine, rounded, isotropic, greenish-blue particles; no birefringence; no pleochroism; appears deep red through Chelsea filter | ASTM lightfastness=1 (excellent); Inert to acids and bases. | chronic inhalation may cause asthma and possible fibrosis |
| chrysocolla | copper silicate, CuSiO3-nH2O |  | naturally occurring blue mineral | 2.4 | 1.575, 1.598, 1.597 | variable ground particles are anisotropic with high birefringence, straight extinction and are pleochroic changing from pale green to colorless | appears green when ground as powder | no significant hazards |
| cobalt blue | cobaltous aluminate, CoO.Al2O3 | Pigment Blue 28; CI 77346 | developed in 1802, sold as artist pigment c. 1820 | 3.83 | 1.662-1.74 | irregular to rounded blue particles, no birefringence, no pleochroism; appears red through Chelsea filter | unaffected by acids, alkalis, light and heat; ASTM lightfastness=1 (excellent) | skin contact may cause allergies. |
| Egyptian blue | double silicate of calcium and copper, CaCuSi4O10 | Pigment Blue 31; CI 77437 | used by Egyptians; later manufactured in Italy |  | e =1.59, w =1.63 | irregular particle shapes; pleochroic from deep blue to colorless; strong birefringence; appears red with Chelsea filter | very stable; insoluble in acids; unaffected by light or heat; ancient Egyptian blue may contain quartz and calcite as impurities | no significant hazards |
| indigo | natural dye from Indigofera tinctoria, C16H10N2O2 | Natural Blue 1; CI 75780 (natural); Pigment Blue 66; CI 73000 (synthetic) | natural indigo used by 4th century; synthetic produced in 1880. |  | >1.662 | fine, translucent dark blue, rounded particles that are weakly birefringent and appear dark red under Chelsea filter | insoluble in water; discolored by reducing agents & bleaches; ISO R105 Lightfastness Classification = 3-4 | no significant hazards |
| manganese blue | BaMnO4-BaSO4 | Pigment Blue 33; CI 77112 | discovered in 1907; marketed as pigment in 1935; production discontinued in 1970s | 4.85 | ~1.65 | rectangular particles with rounded edges; strongly pleochroic from dark to pale turquoise; strong birefringence under crossed polars | ASTM lightfastness=1 (excellent) | toxic by inhalation or ingestion |
| Maya blue | palygorskite clay dyed with indigo |  | used in Mesoamerica since ancient times |  | 1.522-1.548 | fibrous or platy particles are pleochroic (turquoise blue to yellow-green). Weak birefringence under crossed polars. | unaffected by alkalis; soluble in hot concentrated acids |  |
| phthalocyanine blue | copper phthalocyanine, C32H16N8Cu | Pigment Blue 15; CI 74160 | developed in 1933; sold as paint pigment in 1935 | 1.6 | 1.38 | fine grain translucent to opaque particles with moderate to strong birefringence; crystal type I appears deep red through Chelsea filter and crystal type II appears black | slowly turns yellow then dissolves in concentrated sulfuric acid; ASTM lightfastness=2 (very good) | suspected carcinogen, teratogen |
| Prussian blue | ferric ferrocyanide, Fe4[Fe(CN)6]3 | CI Pigment Blue 27; CI 77510 | developed in 1704; first sold as artists' pigment c. 1730 | 1.83 | 1.56 | cubic crystal system; isotropic; very fine particles (0.01 - 0.2 micrometers) appear black under Chelsea filter | ASTM lightfastness=1 (excellent: but often varies with manufacturer). Soluble in acids, decomposes in alkali. | can emit hydrogen cyanide gas if exposed to acids, heat or UV radiation |
| smalt | ground potassium glass, K, Al, Co silicate |  |  |  | 1.46-1.55 | conchoidal fracture, with sharp edges and splinter; no birefringence, no pleochroism; transparent pale blue to deep purple particles | lightfastness is variable; poor covering power; unaffected by acids, alkalis; may have quartz impurities | no significant hazards |
| ultramarine blue, natural | powdered lazurite | Pigment blue 29; CI 77007 | extracted from lapis lazuli as early as the 13th century | 2.4 - 2.5 | about 1.5 | irregular particles, no birefringence, no pleochroism, extinction under crossed polars; naturally mixed with silicates, calcite and pyrite | discolors when exposed to weak acids or sulfur fumes; ASTM lightfastness=1 (excellent) | no significant hazards |
| ultramarine blue, synthetic | 3Na2O.3Al2O3.6SiO2.2Na2S | Pigment Blue 29; CI 77007 | developed in 1826, sold as artist pigment in 1828 | 2.34 | 1.51; 1.63 | small, round uniform particles, no birefringence, no pleochroism, extinct in crossed polars | discolors when exposed to weak acids or sulfur fumes; ASTM lightfastness=1 (excellent) | no significant hazards |
| vivianite | ferrous phosphate, Fe3(PO4)2 - 8H2O |  | naturally occurring mineral used as pigment in 13th/14th c. | 2.58-2.68 | 1.60; 1.63; 1.65 | lath-shaped crystals and fragments with strong birefringence; appears blue-green under Chelsea filter | slowly decomposes and darkens in light and air |  |